## Slide 1
Rolling shear and punching shear of CLT
Houman Ganjali
Ph.D. Candidate, University of Northern British Columbia
A CWCRN Initiative
NSERC Alliance Grant Project ‘NEXT-GENERATION WOOD CONSTRUCTION’

## Slide 2
Dr. Thomas Tannert
Supervisor
Dr. Jianhui Zhou
Supervisory committee member
Dr. Md Shahnewaz
Supervisory committee member
Industry partner
Carla Dickof
Industry partner
Dr. Marjan Popovski
Supervisory committee member

## Slide 3: Content
Cross laminated Timber (CLT)
Point-supported CLT
Punching shear
CLT rolling shear
CLT punching shear
Project outlook

## Slide 4: Cross laminated Timber (CLT)
https://www.reidmiddleton.com/reidourblog/timber-construction-using-clt/

## Slide 5: Point Supported CLT (Post+Plank)
Muster M. and Frangi A. 2020
Photo credit: Fast+Epp
Photo credit: Fast+Epp

## Slide 6: Punching shear in CLT
Photo credit: Dr. Thomas Tannert

## Slide 7: CLT rolling shear strength
CSA O86 rolling shear strength values
Predictors of higher RS strength
Compare test methods
Compare results with punching shear tests

## Slide 8: Modified rolling shear test
EN 408
Mestek’s modifications

## Slide 9: Rolling shear inclined tests
689 specimens
22 series
5 CLT providers
E1 & V2 stress grades
3- & 5-layered layups
4 species (Spruce, SPF, HEM, D-Fir)
Minor and major direction
2 test layer thicknesses
Edge glued and non-edge glued

## Slide 10: Rolling shear inclined test results
CSA O86 RS value: 0.5-0.6 MPa
High RS predictor(s)?
Series | 5th% [MPa] | ADJ [MPa]
S1 | 1.02 | 0.89
S2 | 0.62 | 0.54
S3 | 0.73 | 0.64
S4 | 1.27 | 1.11
S5 | 1.24 | 1.08
S6 | 1.24 | 1.08
S7 | 0.84 | 0.73
S8 | 0.74 | 0.64
S9 | 0.74 | 0.64
S10 | 1.10 | 0.96
S11 | 0.71 | 0.61
S12 | 0.82 | 0.71
S13 | 1.08 | 0.94
S14 | 0.70 | 0.61
S15 | 0.88 | 0.77
S16 | 0.88 | 0.77
S17 | 0.87 | 0.76
S18 | 0.84 | 0.73
S19 | 0.88 | 0.77
S20 | 0.90 | 0.78
S21 | 1.14 | 0.99
S22 | 0.92 | 0.80
CSA RS ×1.1
CSA RS × 2.2

## Slide 11: Rolling shear inclined test results
-CLT provider
-Board width to thickness ratio
Timber species
Edge gluing

## Slide 12: Four- & three-point bending tests
48 Specimens
1.7 m by 0.3 m
E1 stress grade
5-layered CLT
Major and Minor

## Slide 13: Four- & three-point bending tests
Series | Mean [MPa] | 5th% [MPa] | ADJ [MPa]
3pt-y | 1.10 | 0.98 | 0.85
3pt-i | 1.28 | 0.98 | 0.85
4pt-y | 1.47 | 1.20 | 1.04
4pt-i | 1.29 | 1.10 | 0.96
> 0.5-0.6 MPa
Mean RS strength from
modified inclined test
Major 1.62 MPa
Minor 1.14 MPa

## Slide 14: Four- & three-point bending tests
Rolling shear stresses based on simplified and SA methods: major (left); minor(right)
-Simplified method
-Shear analogy (SA) method

## Slide 15: Punching shear tests
Influencing parameters on the punching shear capacity of CLT

## Slide 16: Punching shear test overview
16
Series | Producer | Grade | Thickness [mm] | Species | Support [mm x mm] | Support | Reinforcem.
S1 | D | V2 | 175 | SPF | 200 x 200 | Edge | None
S2 | D | E1 | 175 | SPF | 200 x 200 | Edge | None
S3 | A | E1 | 175 | Spruce | 200 x 200 | Edge | None
S4 | B | E1 | 175 | SPF | 200 x 200 | Edge | None
S5 | B | E1 | 175 | SPF | 300 x 300 | Edge | None
S6 | F | V2 | 175 | SPF | 200 x 200 | Edge | None
S7 | F | E1 | 175 | SPF | 200 x 200 | Edge | None
S8 | F | E1 | 175 | D Fir | 200 x 200 | Edge | None
S9 | F | E1 | 175 | HML | 200 x 200 | Edge | None
S10 | F | E1 | 175 | SPF | 460 x 180 LLP | Edge | None
S11 | F | E1 | 175 | SPF | 460 x 180 SLP | Edge | None
S12 | F | E1 | 175 | SPF | Ø 219 | Edge | None
S13 | F | E1 | 175 | SPF | 200 x 200, 10+ | Edge | None
S14 | F | E1 | 175 | SPF | 200 x 200, 25+ | Edge | None
S15 | F | E1 | 175 | SPF | 300 x 300 | Edge | None
S16 | F | E1 | 175 | SPF | 200 x 200* | Edge | None
S17 | F | E1 | 245 | SPF | 300 x 300 | Edge | None
S18 | F | E1 | 175 | SPF | 200 x 200 | Edge | STS
S19 | F | E1 | 175 | SPF | 200 x 200 | Edge | STS
S20 | F | E1 | 175 | SPF | 200 x 200 | Edge | STS
S21 | F | E1 | 175 | SPF | 400 x 400 | Edge | STS
S22 | F | E1 | 175 | SPF | 200 x 200 | Edge | STS
S23 | F | E1 | 175 | SPF | 200 x 200** | Edge | None
S24 | F | E1 | 175 | SPF | 200 x 200 | Interior | None
S25 | F | E1 | 175 | SPF | Ø 219 | Interior | None
S26 | F | E1 | 175 | SPF | 200 x 200 | Interior | None
S27 | F | E1 | 175 | SPF | 200 x 200 | Interior | None
S28 | F | E1 | 175 | SPF | 200 x 200 | Interior | None
S29 | F | E1 | 245 | SPF | 300 x 300 | Interior | None
S30 | F | E1 | 175 | SPF | 200 x 200 | Perimeter | None
S41 | F | E1 | 175 | SPF | 200 x 200 | Corner | None
S42 | F | E1 | 245 | SPF | 200 x 200 | Corner | None
32 series (so far)
4 provider
2 grades
2 thicknesses
3 species
3 support geometry
4 column conditions
STS reinf. levels

## Slide 17
Edge support
Centre support

## Slide 18
Corner support
Perimeter support

## Slide 19
Column geometry
Square plate + wooden stub
200×200 mm
300×300 mm

## Slide 20
Column geometry
Rectangular + wooden stub
X- and Y-oriented

## Slide 21
Column geometry
Round + stub

## Slide 22
Column geometry
Square plate & NO stub
200×200 mm, low out of plane stiffness
400×400 mm, high out of plane stiffness

## Slide 23
Screw reinforcement design (@45°)
Equivalent RS strength [MPa] =
RS strength of wood
+ Screw contribution to RS
Screw contribution to RS
= screw withdrawal strength
= distance between screws
= distance between screw rows
Reinforcement zone length?
Reinforcement direction?
5 series
Only 2 estimates: 42% and 27%

## Slide 24
CLT punching shear results
Provider B CLT had the highest capacity
D Fir and Hemlock were stronger
E rated series were slightly stronger

## Slide 25
CLT punching shear results
- Round geometry = less stress concentration
- Softer loading plate = higher capacity

## Slide 26
CLT punching shear results
Highest increase 41%:
- Largest reinf. zone
- Both directions
- Tight screw spacing
Important factors:
- Reinf. level
- Reinf. zone
- Reinf. direction

## Slide 27: Project outlook
Long term 4-point bending test

## Slide 28: Project outlook
Full-scale floor tests

## Slide 29: Project outlook
Design guidance for point-supported CLT floors punching shear
Stress distribution model
Adjustment factors
Material related
Support condition related

## Slide 30
Thank You!
Rolling shear and punching shear of CLT
Houman Ganjali
Ph.D. Candidate, University of Northern British Columbia