## Slide 1
A CWCRN Initiative
NSERC Alliance Grant Project ‘NEXT-GENERATION WOOD CONSTRUCTION’
Picture Credit: Alberta WoodWORKS
Burn Through Emissions Comparisons of Dimensional Lumber, CLT, LVL, and Glulam
Presenter: Jan Dabrowski
Affiliation: University of Waterloo
Supervised by Dr. E. Weckman

## Slide 2
Objective of the Study
Methods
Experimental Results
  Evolving Heat Release Rate, Emissions and Timeline
    CLT
    Glulam
    Dimensional Lumber
    LVL
Conclusion
  Study Findings
Overview

## Slide 3
To improve the understanding of the following for engineered wood products (CLT, LVL, and Glulam):
  Emissions
  Charring Mechanism
  Evolving Heat Release Rate
To investigate the differences between wood products that contain glues or resins to wood products without them:
  Utilizing SPF dimensional lumber as a wood product baseline that contains no glues or resins.
Objective of the Study

## Slide 4
Cone Calorimeter
  HRR
  O2
  CO2
  CO
Gas Sampling Instrumentation
  NH3
  CH4
  VOC
Methods
Sampling Line
Pump
Gas Sampling Instrumentation
Exhaust Line

## Slide 5
Specimens of 10 cm x 10 cm x 1 cm are cut from dimensional lumber, CLT, LVL, and Glulam.
CLT and Glulam specimens are cut such that the maximum amount of glue lines are exposed to the radiant heat flux.
An initial probe into whether any different gases from the glue could be seen.
Methods
CLT
LVL
Glulam
Dimensional Lumber

## Slide 6
Two of each sample type is tested under 35 kW/m2 and 50 kW/m2 flux.
Tested from ignition to burn through under well-ventilated conditions.
Methods
CLT Sample Before:
35 kW/m2 Radiant Heat Flux Exposure
Ignition
Flameout
CLT Sample After:
35 kW/m2 Radiant Heat Flux Exposure

## Slide 7
Experimental Results: CLT – HRR & Oxygen
HRR and oxygen depletion for CLT is observed to have a double peaked behavior.
Double peak behavior is observed for both heat fluxes.

## Slide 8
CLT, Dimensional Lumber, Glulam – HRR
Similar double peak behavior in HRR is observed for:
  Glulam
  Dimensional Lumber
CLT and Dimensional Lumber appear to have similar HRR Trends.
A period of steady HRR is observed for Glulam prior to peaking again.

## Slide 9
CLT, Dimensional Lumber, Glulam – Oxygen

## Slide 10
CLT, Dimensional Lumber, Glulam – CO2

## Slide 11
CLT, Dimensional Lumber, Glulam – CO

## Slide 12
CLT, Dimensional Lumber, Glulam – VOC

## Slide 13
CLT, Dimensional Lumber, Glulam – Ammonia (NH3)

## Slide 14
CLT, Dimensional Lumber, Glulam – Methane (CH4)

## Slide 15
Burn Through Timeline: CLT – 50 kW/m2
Visible
Smoke
Increase in
Smoke Intensity
Fully Charred Surface
Ignition
Sample 2:
Start of Arching
Sample 1:
End of Arching
Sample 1:
Start of Arching
Sample 1:
Flameout
Sample 2:
End of Arching
Sample 2:
Flameout

## Slide 16
Burn Through Timeline: Glulam – 50 kW/m2
Visible Smoke
Increase in
Smoke Intensity
Fully Charred Surface
Sample 2:
Start of Arching
Sample 1:
End of Arching
Sample 1:
Start of Arching
Sample 1:
Flameout
Sample 2: End of Arching
Sample 2:
Flameout
Ignition

## Slide 17
Burn Through Timeline: Dimensional Lumber – 50 kW/m2
Visible Smoke
Increase in
Smoke Intensity
Fully
Charred Surface
Ignition
Sample 2:
Start of
Arching
Sample 1: End of Arching
Sample 1:
Start of Arching
Sample 1: Flameout
Sample 2:
End of Arching
Sample 2: Flameout
Sample 1: Peak Bowing
Sample 1: Return to Normal

## Slide 18
Experimental Results: LVL – HRR & Oxygen

## Slide 19
Experimental Results: LVL – O2 & CO2

## Slide 20
Experimental Results: LVL – O2 & CO

## Slide 21
Experimental Results: LVL – VOC & CH4

## Slide 22
Experimental Results: LVL – HRR & NH3

## Slide 23
Burn Through Timeline: LVL – 50 kW/m2
Sample 1: Start Of Arching
Sample 1: End of Arching
Sample 1: Flameout
Sample 2: End of Arching
Sample 2: Flameout
Ignition
Sample 2:
Peak
Bowing
Sample 1:
Peak Bowing
Sample 2
Start Of
Arching

## Slide 24
Burn Through Timeline: LVL – 35 kW/m2
Increase in
Smoke Intensity
Fully
Charred Surface
Sample 2:
Start Of Arching
Sample 1:
End of Arching
Sample 1: Flameout
Sample 2: End of Arching
Sample 2: Flameout
Ignition
Visible Smoke
Sample 2:
Peak Bowing
Sample 1: Peak Bowing
Sample 2:
Return to
Normal
Sample 1: Return to Normal
Sample 1: Start Of Arching

## Slide 25
This initial investigation has revealed that for CLT and Glulam no differences in gases from the glue could be seen.
The evolving heat release rate and emissions (O2, CO2, and CO) for Glulam and CLT follow similar trends as dimensional lumber.
LVL has a different evolving heat release rate and emissions (O2, CO2, CO, and VOC).
The VOC, CH4, and NH3 all peak approximately at ignition and then peak for a second time near flameout:
  VOC and NH3 from LVL are exceptions to this trend.
  NH3 from Glulam is an exceptions to this trend.
CLT, Glulam, LVL, and dimensional lumber are observed to either arch or bow at different times.
Conclusion – Study Findings

## Slide 26
Government Partners

## Slide 27
Research Partners

## Slide 28
Industry Partners

## Slide 29
Questions?